## Slide 1: ColyFloor 2500FC UV Resistance Polyurethane Coating
Product Description
ColyFloor 2500FC is a two-component, chemically cured, recoatable aliphatic polyurethane topcoat known for its exceptional UV resistance and durability. This high-solids, UV-resistant topcoat provides excellent mechanical and chemical resistance along with superior gloss retention. Once cured, the film offers robust protection against heavy traffic and mechanical wear, with high resistance to abrasion and impact. It is commonly used as a protective topcoat in the ColyFoor floor protection systems where maximum protection is essential. Typical applications include car park decks, aircraft hangars, chemical processing plants, and offshore structures.
Product Information |  | 
Finish | : | High Gloss
Color | : | Wide Range of Color
Flashpoint | : | > 25 °C
Volume Solids | : | 50 ±2%
Specific Gravity | : | 1.05 -1.25 gm/cm³ (depend by colour)
Abrasion Resistance | : | 30mg/1000 cycles (ASTM D4060 – CS 17)
Pot Life (30°C) | : | 1.5 – 2 hours
Recoat Time | : | Min. 16 hours at 25 °C, Max unlimited at 25 °C
Curing Times (25°C) | : | After 24 hours (for light traffic), After 7 days (full cure for heavy services)
Maxing Ratio (A/B) | : | 83 / 17 by weight
Consumption | : | 4 – 5 m² /L
Recommended DFT | : | 80 – 120 µm
Thinning | : | Thinner C 50
Packing | : | 5L & 20L /set
Shelf Life & Storage (unopened and in good conditions temperature 10°C - 30°C) | : | 12 months
Technical Data Sheet
Typical System for Concrete Floor |  | 
Coating Sequence |  | Product Name
Primer | : | ColyFloor 5000PM
Second Coat | : | ColyFloor 2500FC
Finish Coat | : | ColyFloor 2500FC
COLY COAITNG SDN BHD
1 No. 421-B Batu 14, Jalan Kapar, 42200 Kapar Klang, Selangor Darul Ehsan
Tel.603 3259 3905; Fax. 603 3259 3904; e-mail sales@colycoating.com.my ; Web-site : www.colycoating.com.my
Benefits
Excellent weathering resistant against UV degradation
High abrasion resistance and excellent chemical resistance
Hygienic, easy to take care
Seamless, monolithic application
Available in wide range of colour

## Slide 2
COLY COAITNG SDN BHD
1 No. 421-B Batu 14, Jalan Kapar, 42200 Kapar Klang, Selangor Darul Ehsan
Tel.603 3259 3905; Fax. 603 3259 3904; e-mail sales@colycoating.com.my ; Web-site : www.colycoating.com.my
Technical Data Sheet
Shubstrate Requirement & Preparation
Substrate concrete screed should a minimum of compressive strength 25N/mm² and adhesive pull-off strength of minimum 1.5N/mm² (concrete failure). New concrete floor should be a minimum of 28 days and must be dry to below a moisture content of 4%. For adequate adhesion of coatings to concrete surface should be free of laitance. Oil, grease, dust, paint residues, algae, loose and friable material must be completely removed form all surface before application the product.
Rough contaminations and high spots can be remove by grinding. Concrete substrates must be prepared mechanically using abrasive blast cleaning or scarifying equipment to remove cement laitance and a achieved on open texture surface. Surface must be dry and free from any leakage source. All surface cracks, damage concrete surface must first be repair with ColyFloor epoxy repair compound.
Safety Precaution
This product is flammable and must be kept away from any source of ignition. Use under well ventilated conditions. Do not breathe or inhale mist. Avoid skin contact. Spillage on the skin should immediately be removed with suitable cleanser, soap and water. Eyes should be well flushed with water and medical attention sought immediately. Keep out of reach of children.
Disclaimer: The above information is given to the best of our knowledge based on laboratory tests and practical experience. However, since we cannot anticipate or control the many conditions under which our product by be used, we can only guarantee the quality of the product itself. We reserve the right to alter the given data without prior notice.
REV Date: Dec 2023
Technical Data Sheet – ColyFloor 2500FC
Maxing And Application
Pour total Part B in the Part A container and mix both liquid part thoroughly for one minute by using a suitable electrical stirrer (with 750 watt high power mixer) until a fully homogenous mix has bee achieved. Than slowly add 5% - 10% thinner 50 (if need) while mixing continues for a further 1 minute 30 second until a full homogenous mix has been achieved.
Apply ColyFloor 2500FC can be use by suitable roller, brush or trowel and overwork with a roller.
Apply ColyFloor 2500FC within the pot life (working time),
Do not apply when the relative humidity exceed 90% on when the surface to be coated is less than 5% above the dew point.
Do not apply temperature below 5°C and temperature above 40°C
Maintenance and care after cure
Recommend basic cleaning and maintenance will prolong the life of epoxy floors, clean regularly using a single or double headed rotary scrubber drier in conjunction with alkaline detergent.