## Slide 1: ColyFloor 3000MT Epoxy Mortar
Product Description
ColyFloor 3000MT is a three – part compound designed for underlayment applications. It comprises modified epoxy resin, a polyamide hardener, and graded aggregate enable prevent osmotic blistering in resin-based floor finishes . It highly recommended for creating a moisture protection barrier over damp concrete floors and also used for environments requiring a extremely tough industrial grade flooring.
Product Information |  | 
Finish | : | Matt
Color | : | Natural
Volume Solids | : | 100 %
Specific Gravity | : | 2.0±0.2 gm/cm³
Tensile Adhesion (Pull-Off Strength) | : | 2 N/mm² failure in concrete (ASTM D4541)
Tensile Strength | : | 14N/mm² (ASTM C307)
Compressive Strength | : | 90 N/mm² (ASTM C579)
Abrasion Resistance | : | 30mg/1000 cycles (ASTM D4060 – CS 17)
Pot Life (30°C) | : | Approx. 40 Mins
Curing Times (25°C) | : | After 24 hours (for light traffic), After 7 days (full cure for heavy services)
Consumption | : | 1.9 -2.0kg/m²/mm
Packing | : | 55kg /set (A+B+C)
Thinning | : | Do not thin
Shelf Life & Storage (unopened and in good conditions temperature 10°C - 30°C) | : | 12 months
Technical Data Sheet
Typical System for Concrete Floor |  | 
Coating Sequence |  | Product Name
Primer | : | ColyFloor 6000PM
Underlayment | : | ColyFloor 3000MT
Finish Coat | : | ColyFloor 6500FC or ColyFloor 6510SL
COLY COAITNG SDN BHD
1 No. 421-B Batu 14, Jalan Kapar, 42200 Kapar Klang, Selangor Darul Ehsan
Tel.603 3259 3905; Fax. 603 3259 3904; e-mail sales@colycoating.com.my ; Web-site : www.colycoating.com
Benefits
Outstanding toughness with hard wearing and impact resistance
Good physical strength
Specially blend aggregate engineered for quicker, easier and tighter trowel ability.
High levels of chemical resistance to fuels and lubricants, most solvents and chemicals.
Solvent free, low odour.
User friendly

## Slide 2
COLY COAITNG SDN BHD
1 No. 421-B Batu 14, Jalan Kapar, 42200 Kapar Klang, Selangor Darul Ehsan
Tel.603 3259 3905; Fax. 603 3259 3904; e-mail sales@colycoating.com.my ; Web-site : www.colycoating.com.my
Technical Data Sheet
Shubstrate Requirement & Preparation
Substrate concrete screed should a minimum of compressive strength 25N/mm² and adhesive pull-off strength of minimum 1.5N/mm² (concrete failure). New concrete floor should be a minimum of 28 days and must be dry to below a moisture content of 4%. For adequate adhesion of coatings to concrete surface should be free of laitance. Oil, grease, dust, paint residues, algae, loose and friable material must be completely removed form all surface before application the product.
Rough contaminations and high spots can be remove by grinding. Concrete substrates must be prepared mechanically using abrasive blast cleaning or scarifying equipment to remove cement laitance and a achieved on open texture surface. Surface must be dry and free from any leakage source. All surface cracks, damage concrete surface must first be repair with ColyFloor epoxy repair compound.
Safety Precaution
This product is flammable and must be kept away from any source of ignition. Use under well ventilated conditions. Do not breathe or inhale mist. Avoid skin contact. Spillage on the skin should immediately be removed with suitable cleanser, soap and water. Eyes should be well flushed with water and medical attention sought immediately. Keep out of reach of children.
Disclaimer: The above information is given to the best of our knowledge based on laboratory tests and practical experience. However, since we cannot anticipate or control the many conditions under which our product by be used, we can only guarantee the quality of the product itself. We reserve the right to alter the given data without prior notice.
REV Date: Dec 2023
Technical Data Sheet – ColyFloor 3000MT
Maxing And Application
Pour total Part B into the Part A container and mix both liquid part thoroughly for one minute by using suitable electrical stirrer (with 750 watt high power mixer) until a fully homogenous mix has been achieved, transfer Part A & Part B (mixed) to a forced action mixer e.g a crete angle and mix with aggregate(Part C) until uniform.
Apply ColyFloor 6000PM as a primer for sealing well the substrate porosity 80 µm – 100 µm.
Usually within 8 -14 hours, ColyFloor 6000PM cured. Apply the mixed ColyFloor 3000MT , with 1 hours of priming (i.e. while the priming coat is still tacky), and spread the screed onto the primer floor with screed box as per requirement thickness, compact and finish using a steel blade trowel or power float.
Do not apply when the relative humidity exceed 90% on when the surface to be coated is less than 5% above the dew point.
Do not apply temperature below 5°C and temperature above 40°C
Maintenance and care after cure
Recommend basic cleaning and maintenance will prolong the life of epoxy floors, clean regularly using a single or double headed rotary scrubber drier in conjunction with alkaline detergent.