## Slide 1: ColyFloor 6000PM Solvent Free Epoxy Primer
Product Description
ColyFloor 6000PM is a high performance two components solvent-free epoxy primer/sealer. It is low viscosity, 100% solids epoxy penetrating primer/sealer with specially formulated to reduce the rate of moisture vapour transmission from the concrete floor to an acceptable levels prior to the installation of the resin toppings. It usually used together with ColyFloor 3000MT, epoxy mortar screed to provide a highly effective heavy duty moisture barrier protection against excessive moisture in the concrete substrate.
Product Information |  | 
Finish | : | Glossy
Color | : | Clear
Flashpoint | : | > 65 °C
Volume Solids | : | 100 %
Specific Gravity | : | 1.08 ± 0.2kg/L
Tensile Adhesion (Pull-Off Strength) | : | 2 N/mm² failure in concrete (ASTM D4541)
Pot Life (30°C) | : | Approx. 35 Mins
Tough Dry (30°C) | : | 7 hours
Recoating Time | : | Min. 16 hours at 25°C, Max 48 hours at 25°C
Curing Times (25°C) | : | After 24 hours (for light traffic), After 7 days (full cure for heavy services)
Consumption | : | 9 -12/m²/L
Packing | : | 5L (A: 3.39L ; B: 1.61L) 20L (A: 13.55L ; B: 6.45L)
Thinning | : | Do not thin
Shelf Life & Storage (unopened and in good conditions temperature 10°C - 30°C) | : | 12 months
Technical Data Sheet
Typical System for Concrete Floor |  | 
Coating Sequence |  | Product Name
Primer | : | ColyFloor 6000PM
Second Coat | : | ColyFloor 6500FC or ColyFloor 3000MT
Finish Coat | : | ColyFloor 6500FC or ColyFloor 6510SL
COLY COAITNG SDN BHD
1 No. 421-B Batu 14, Jalan Kapar, 42200 Kapar Klang, Selangor Darul Ehsan
Tel.603 3259 3905; Fax. 603 3259 3904; e-mail sales@colycoating.com.my ; Web-site : www.colycoating.com.my
Benefits
Low viscosity, good penetrative properties
Excellent adhesion
High levels of chemical resistance to fuels and lubricants, most solvents and chemicals.
Solvent free, low odour.
User friendly

## Slide 2
COLY COAITNG SDN BHD
1 No. 421-B Batu 14, Jalan Kapar, 42200 Kapar Klang, Selangor Darul Ehsan
Tel.603 3259 3905; Fax. 603 3259 3904; e-mail sales@colycoating.com.my ; Web-site : www.colycoating.com.my
Technical Data Sheet
Shubstrate Requirement & Preparation
Substrate concrete screed should a minimum of compressive strength 25N/mm² and adhesive pull-off strength of minimum 1.5N/mm² (concrete failure). New concrete floor should be a minimum of 28 days and must be dry to below a moisture content of 4%. For adequate adhesion of coatings to concrete surface should be free of laitance. Oil, grease, dust, paint residues, algae, loose and friable material must be completely removed form all surface before application the product.
Rough contaminations and high spots can be remove by grinding. Concrete substrates must be prepared mechanically using abrasive blast cleaning or scarifying equipment to remove cement laitance and a achieved on open texture surface. Surface must be dry and free from any leakage source. All surface cracks, damage concrete surface must first be repair with ColyFloor epoxy repair compound.
Safety Precaution
This product is flammable and must be kept away from any source of ignition. Use under well ventilated conditions. Do not breathe or inhale mist. Avoid skin contact. Spillage on the skin should immediately be removed with suitable cleanser, soap and water. Eyes should be well flushed with water and medical attention sought immediately. Keep out of reach of children.
Disclaimer: The above information is given to the best of our knowledge based on laboratory tests and practical experience. However, since we cannot anticipate or control the many conditions under which our product by be used, we can only guarantee the quality of the product itself. We reserve the right to alter the given data without prior notice.
REV Date: Dec 2023
Technical Data Sheet – ColyFloor 6000PM
Maxing And Application
Pour total Part B in the Part A container and mix both liquid part thoroughly for one minute by using a suitable electrical stirrer (with 750 watt high power mixer) until a fully homogenous mix has bee achieved.
Apply ColyFloor 6000PM can be use by suitable roller, brush or trowel and overwork with a roller.
ColyFloor 6000PM should apply within the pot life times at 28°C
Substrate temperature should not apply below 5°C and temperature above the dew point.
Maintenance and care after cure
Recommend basic cleaning and maintenance will prolong the life of epoxy floors, clean regularly using a single or double headed rotary scrubber drier in conjunction with alkaline detergent.