## Slide 1: ColyFloor 6510SL Self-Leveling Epoxy Floor Coating
Product Description
ColyFloor 6510SL is a high performance two components solvent-free 1mm – 3mm self-leveling covering compound of high grade epoxy resin floor coating. It provides a tough and smooth epoxy floor surface covering for industrial floors with good water, chemical and abrasion resistance. It recommended for application on areas where clean, chemical resistance and hard wearing resistance floor finish is required. It widely used for factories, automotive industries, workshop, production clean room, schools, pharmaceutical plants, food processing plant and hospital etc.
Product Information |  | 
Finish | : | Glossy
Color | : | Wide Range of Color
Flashpoint | : | > 24 °C
Volume Solids | : | 100 %
Specific Gravity | : | 1.35 ± 0.2kg/L
Tensile Adhesion (Pull-Off Strength) | : | 2 N/mm² failure in concrete (ASTM D4541)
Tensile Strength | : | 20 MPA (ASTM C307-03)
Compressive Strength | : | 56 MPA(ASTM C570-01)
Abrasion Resistance | : | 15 mg / 1000 cycles (ASTM D4046)
Pot Life (30°C) | : | Approx. 35 Mins
Mechanical Curing | : | 24 hours
Curing Times (25°C) | : | After 24 hours (for light traffic), After 7 days (full cure for heavy services)
Maxing Ratio (A/B) | : | 80/20 by weight
Consumption | : | 1L (1.35kg -1.45kg)/m²/1mm
Packing | : | 5L & 20L /set
Thinning | : | Do not thin
Shelf Life & Storage (unopened and in good conditions temperature 10°C - 30°C) | : | 12 months
Technical Data Sheet
Typical System for Concrete Floor |  | 
Coating Sequence |  | Product Name
Primer | : | ColyFloor 6000PM
Finish Coat | : | ColyFloor 6510SL
COLY COAITNG SDN BHD
1 No. 421-B Batu 14, Jalan Kapar, 42200 Kapar Klang, Selangor Darul Ehsan
Tel.603 3259 3905; Fax. 603 3259 3904; e-mail sales@colycoating.com.my ; Web-site : www.colycoating.com.my
Benefits
Outstanding toughness with hard wearing and impact resistance.
Seamless and hygienic floor finishes with no crevices where dirt and bacteria can dwell.
High levels of chemical resistance to fuels and lubricants, most solvents and chemicals.
Solvent free, low odour.
Low maintenance with easy to clean and sterilize.

## Slide 2
COLY COAITNG SDN BHD
1 No. 421-B Batu 14, Jalan Kapar, 42200 Kapar Klang, Selangor Darul Ehsan
Tel.603 3259 3905; Fax. 603 3259 3904; e-mail sales@colycoating.com.my ; Web-site : www.colycoating.com.my
Technical Data Sheet
Shubstrate Requirement & Preparation
Substrate concrete screed should a minimum of compressive strength 25N/mm² and adhesive pull-off strength of minimum 1.5N/mm² (concrete failure). New concrete floor should be a minimum of 28 days and must be dry to below a moisture content of 4%. For adequate adhesion of coatings to concrete surface should be free of laitance. Oil, grease, dust, paint residues, algae, loose and friable material must be completely removed form all surface before application the product.
Rough contaminations and high spots can be remove by grinding. Concrete substrates must be prepared mechanically using abrasive blast cleaning or scarifying equipment to remove cement laitance and a achieved on open texture surface. Surface must be dry and free from any leakage source. All surface cracks, damage concrete surface must first be repair with ColyFloor epoxy repair compound.
Safety Precaution
This product is flammable and must be kept away from any source of ignition. Use under well ventilated conditions. Do not breathe or inhale mist. Avoid skin contact. Spillage on the skin should immediately be removed with suitable cleanser, soap and water. Eyes should be well flushed with water and medical attention sought immediately. Keep out of reach of children.
Disclaimer: The above information is given to the best of our knowledge based on laboratory tests and practical experience. However, since we cannot anticipate or control the many conditions under which our product by be used, we can only guarantee the quality of the product itself. We reserve the right to alter the given data without prior notice.
REV Date: Dec 2023
Technical Data Sheet – ColyFloor 6510SL
Maxing And Application
Pour total Part B in the Part A container and mix both liquid part thoroughly for one minute by using a suitable electrical stirrer (with 750 watt high power mixer) until a fully homogenous mix has bee achieved.
Apply ColyFloor 6000PM as 1st coat primer on well prepare surface by good quality medium pile lamb wool roller then allowed to cure within 8-14 hours prior to application of ColyFloor 6510SL.
Apply ColyFloor 6510SL within the pot life (working time), spread the composite matrix with notched squeegee or pin rake and set it to the correct depth or requirement thickness. Immediately release the air/bubble by using spike roller.
Do not apply when the relative humidity exceed 90% on when the surface to be coated is less than 5% above the dew point.
Do not apply temperature below 5°C and temperature above 40°C
Maintenance and care after cure
Recommend basic cleaning and maintenance will prolong the life of epoxy floors, clean regularly using a single or double headed rotary scrubber drier in conjunction with alkaline detergent.